Methodical evaluation and improvement of matrix compatible PDMS-overcoated coating for direct immersion solid phase microextraction gas chromatography (DI-SPME-GC)-based applications

Érica A. Souza-Silvaaψ, Emanuela Gionfriddoa, Robert Shirey b, Len Sidiskyb, Janusz Pawliszyna*.

a Department of Chemistry, University of Waterloo, 200 University Avenue West, Waterloo, Ontario, Canada N2L 3G1

b Supelco Inc., 595 North Harrison Road, Bellefonte, PA 16823, USA

ψ Current address: Instituto de Química, Universidade Federal do Rio Grande do Sul (UFRGS), Av. Bento Gonçalves, 9500, 91501-970 Porto Alegre-RS, Brazil.

*Corresponding author’s name: Janusz Pawliszyn

Corresponding author’s phone number: 1-519-888-4567 ext. 84641

Corresponding author’s fax number: 1-519-746-0435

Corresponding author’s e-mail: janusz@sciborg.uwaterloo.ca

Supporting Information

Table S1 - Model analytes in standard mixture for coating evaluation.

|  | Working Mixture ( µg/mL) | Log P (pH 7) | MW (g/mole) | Quant. Ion (m/z) |
| --- | --- | --- | --- | --- |
| Nitrobenzene | 50 | 1.90 | 123 | 77 |
| 1,3-Dinitrobenzene | 150 | 1.43 | 168 | 168 |
| 2,6-Dinitrotoluene | 75 | 2.42 | 182 | 165 |
| Trifluralin | 5 | 5.07 | 325 | 306 |
| 4-Phenylphenol | 20 | 3.20 | 170 | 170 |
| Diazinon | 7.5 | 3.40 | 304 | 304 |
| Chlorothalonil | 15 | 2.94 | 266 | 266 |
| Parathion | 5 | 3.83 | 291 | 291 |
| Pendimethalin | 5 | 5.18 | 281 | 252 |
| p,p'-DDE | 2.5 | 6.00 | 318 | 318 |
| Diazepam | 100 | 2.80 | 284 | 256 |

Figure S1 - Structures of model analytes employed in the current coating evaluation.

Figure S2 - Representative chromatogram: analytes from standard mixture extracted from water using commercial PDMS/DVB fiber.

Figure S3 - pH and salt (%) dependence of the amount extracted by a PDMS/DVB fiber from grape juice samples.

Figure S4 - pH and salt (%) dependence of the amount extracted by a PDMS/DVB fiber from water samples.

Figure S5 - Nitrobenzene: reusability profile of coatings subjected to 40 DI-SPME in Concord grape juice.

Figure S6 - 2,6-Dinitrotoluene: reusability profile of coatings subjected to 40 DI-SPME in Concord grape juice.

Figure S7 - Trifluralin: reusability profile of coatings subjected to 40 DI-SPME in Concord grape juice.

Figure S8 - 4-Phenylphenol: reusability profile of coatings subjected to 40 DI-SPME in Concord grape juice.

Figure S9 - Diazinon: reusability profile of coatings subjected to 40 DI-SPME in Concord grape juice.

Figure S10 - Chlorothalonil: reusability profile of coatings subjected to 40 DI-SPME in Concord grape juice.

Figure S11 - p,p'-DDE: reusability profile of coatings subjected to 40 DI-SPME in Concord grape juice.

Figure S12 - Diazepam: reusability profile of coatings subjected to 40 DI-SPME in Concord grape juice.

Figure S13 - Diazinon stability test in water matrix.

Figure S14 - Comparison of RSDs throughout 40 extractions in grape juice sample.

Table S2 - Intra-fiber: paired two samples for means (for each fiber, comparing the first 20 and last 20 extractions).

| Paired t-test for means |  |  |  |  |
| --- | --- | --- | --- | --- |
|  | PDMS/DVB | GC-PDMS 30µm | GC-PDMS 10 µm | Sylgard 30 µm |
| Nitrobenzene | No | No | Yes | Yes |
| 1,3-Dinitrobenzene | No | No | No | Yes |
| 2,6-Dinitrotoluene | No | No | No | Yes |
| Trifluralin | No | No | No | Yes |
| 4-Phenylphenol | No | No | No | Yes |
| Chlorothalonil | No | No | No | No |
| Parathion | No | No | No | No |
| Pendimethalin | No | No | No | No |
| p,p’-DDE | No | Yes | Yes | No |
| Diazepam | No | No | No | No |

Table S3 - Inter-fiber: two-sample assuming unequal or equal variances (n=100, except PDMS/DVB n=60)).

| Two sample t-test |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Syl/ GC30µm | Syl/ GC10µm | Syl/ PDMS/DVB | GC30µm/ PDMS/DVB | GC10µm/ PDMS/DVB | GC30µm/ GC10µm |
| Nitrobenzene | No | No | No | No | No | Yes |
| 1,3-Dinitrobenzene | No | No | No | No | No | No |
| 2,6-Dinitrotoluene | No | No | No | Yes | Yes | Yes |
| Trifluralin | No | No | No | No | No | Yes |
| 4-Phenylphenol | No | No | No | Yes | Yes | Yes |
| Chlorothalonil | No | No | No | No | No | Yes |
| Parathion | No | No | No | No | No | No |
| Pendimethalin | No | No | No | No | No | Yes |
| p,p’-DDE | No | No | No | No | No | No |
| Diazepam | Yes | No | No | No | Yes | No |

PDMS/DVB

GC- PDMS 10 µm

Sylgard 30 µm

Figure S15 - Microscopic pictures of coatings after 60 extractions in grape juice.

GC-PDMS 30 µm

Sylgard 30 µm

GC- PDMS 30 µm

Figure S16 - Overcoated fiber tips.

Sylgard θ 109.73º

GC-PDMS θ 77.99º

Figure S17 – Water contact angle images for both types of PDMS obtained by measuring the contact angle of 30 µL water drops according to the sessile drop method. Images were acquired every 2 s over a 10 min period, and repeated three times. Contact angle measurements were collected using Axisymmetric Drop Shape Analysis (ADSA).

A

B

C

D

E

F

G

H

I

J

Figure S18 - Reusability profile of coatings subjected to 60 DI-SPME in Concord grape juice.

A

B

A

B

Figure S19 - SEM images of the PDMS-modified coatings: (A) Sylgard sealed end 200x magnification; (B) Partially sealed GC-PDMS end using 500x magnification.

Figure S20 - Pictures depicting an effective PDMS overcoating of coating/metal junction.